Tableau

|  | Competitor | We have |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- |
|  | Ipe | Myanmar Teak (we have for big plank only) | Thaï Teak | Malaysian Teak | Merbau | Chengal |
| Origin | South America | Myanmar | Thaïland | Malaysia | Southeast Asia, Pacific region | Malaysia, Indonesia |
| Density (kg/m³) | 1050–1120 | 600–750 | 620-680 | 550-630 | 830–880 | 900–1050 |
| Janka Hardness (N) | ~14,400 | ~5,900 | ~5,600 | ~5,200 | ~7,600 | ~12,000 |
| Durability | Exceptional (Class 1) | Excellent (Class 1) | Excellent (Class 1) | Excellent (Class 1) | Very Good (Class 2) | Exceptional (Class 1) |
| Moisture Resistance | Excellent | Excellent (natural oils) | Excellent (natural oils) | Excellent (natural oils) | Very Good | Excellent |
| Color | Dark brown / chocolate brown | Golden brown to medium brown | Medium golden / light brown | Pale yellow / Light brown | Reddish-brown with yellow veins | Dark brown with greenish undertones |
| Stability | Very Good | Excellent | Excellent | Excellent | Good | Very Good |
| Workability | Difficult (extremely hard) | Easy | Easy | Easy | Moderate | Difficult |
| Lifespan outside | 50–75 years | 40–60 years | 40–50 years | 40–50 years | 30–50 years | 50–80 years |
| Common Uses | Decking, bridges, cladding | Furniture, boat building, decking | Furniture, boat building, decking | Furniture, boat building, decking | Decking Flooring, joinery, outdoor structures | Framing, bridges, marine construction |